DATA

Candidate papers were found and a review[1]. We included RH or temperature sweeps of single MoS₂-based NO₂ sensors at fixed NO₂ concentration and illumination with readable, internally consistent values, ranked by similarity to our sensor (Au on MoS₂, illumination, room temperature, resistance rising in NO₂). Of 20 sources read, 11 papers qualified[2–12]. Values came from the text, tables or were digitised from figures [software] (uncertainty 1–6%); all but three were independently re-checked.

All responses were converted to one definition,

S=RhighRlow-1×100%                                                                                                   (1)

where Rhigh and Rlow are the larger and smaller of the baseline (Ra) and gas (Rg) resistances; for our rising-resistance sensor, Eq. (1) equals the usual (Rg − Ra)/Ra × 100%. Responses of falling-resistance sensors reported as S′ = (Ra − Rg)/Ra × 100% were converted with

S=S'100-S'×100%                                                                                                (2)

S therefore exceeds 100% when one resistance is more than twice the other: directly for refs 4 and 5 (108–129%), and through Eq. (2) for ref 11, whose 72% decrease at 50 °C becomes 257%.

Each sweep at one NO₂ concentration forms a curve. The RH set has 25 points on six curves from five papers; the temperature set has 58 points on 16 curves from six sensors in five papers[8–12] , four from one laboratory, all measured in the dark (Table 1). One RH paper[2]  was excluded: its responses (500–850%) are 12–20 times ours, and its rise with humidity reflects baseline drift. Each set was padded to 100 rows by log-linear interpolation within measured curves (75 RH, 42 temperature rows) for denser training targets; interpolated rows never trained a model tested on them.

Table 1. Published sweeps used to train the models. S: unified response, Eq. (1); Eq. (2): converted from a falling-resistance response.

| Set | Source | Sensing layer | Fixed conditions | Sweep (points) | S (%) | Conversion |
| --- | --- | --- | --- | --- | --- | --- |
| RH | Hu et al. 2023[3] | Au@MoS₂ core–shell | 1 ppm NO₂; white LED, 4.1 mW cm⁻²; 25 °C | 30–90% RH (4) | 20.3–23.1 | Eq. (2) |
| RH | Hu et al. 2025[4] | Au@MoS₂/SnS | 1 ppm; white LED, 5 mW cm⁻²; 25 °C | 30–70% RH (3) | 108.5–128.6 | as published |
| RH | Li et al. 2026[5] | Au on S-vacancy-rich MoS₂ | 50 ppb; Xe lamp >420 nm, 0.71 mW cm⁻²; 25 °C | 0–80% RH (5) | 107.8–120.6 | as published (current) |
| RH | Li et al. 2026[5] | S-vacancy-rich MoS₂ | as above | 0–80% RH (5) | 14.5–33.6 | as published (current) |
| RH | Ni et al. 2024[6] | Au NPs on exfoliated MoS₂ | 0.5 ppm; dark; 30 °C | 10–90% RH (5) | 1.22–2.29 | Eq. (2) |
| RH | Kumar et al. 2025[7] | MoS₂ sputtered on ZnO nanorods | 0.5 ppm*; 365 nm UV*; 27 °C | 25–85% RH (3) | 6.5–34.6 | as published* |
| T | Ni et al. 2023[8] | exfoliated MoS₂ | 1 ppm; dark; 30% RH; N₂ carrier | 30–100 °C (3) | 1.42–2.15 | Eq. (2) |
| T | Kumar et al. 2018[9] | MoS₂ nanowire network | 1, 2, 3, 5 ppm (4 curves); dark; vacuum chamber | 25–120 °C (12) | 2.52–18.1 | as published |
| T | Kumar et al. 2018[10] | vertically aligned MoS₂ | 1, 5, 10, 20, 50 ppm (5 curves); dark; Ar/N₂ | 25–150 °C (18) | 2.28–46.2 | as published |
| T | Kumar et al. 2018[10] | horizontally aligned MoS₂ | 5, 10, 20, 50 ppm (4 curves); dark; Ar/N₂ | 25–150 °C (16) | 0.86–26.1 | as published |
| T | Kumar et al. 2019[11] | rGO on S-vacancy vertically aligned MoS₂ | 50 ppm; dark; Ar/N₂ | 25–150 °C (4) | 31.6–257.1 | Eq. (2) |
| T | Kumar et al. 2026[12] | CVD MoS₂ film | 20 ppm; dark; dry air | 50–150 °C (5) | 9.6–16.6 | Eq. (2)† |

*Inferred from the paper (neither is a model input); values used as plotted, as the printed formula does not reproduce them. †Treated as falling resistance, as the published transients show, although the text says it rises (if rising, temperature ratios change by <10%).